Setalux D A XP2588

An acrylic polyol with 3.1% OH (calculated on non-volatiles)

丙烯酸多元醇3.1%羟基含量（以固体份计）

Technical features技术特性

Excellent chemical resistance, chalk resistance, good light fastness,and good gloss retention

优秀的耐化学性，抗粉化，耐候性。很好的保光性。

Application应用

In combination with aliphatic polyurethane for 2kPU clear coat and colour lacquers,  industrial topcoats.

与脂肪族聚氨酯合用做双组份聚氨酯清面漆,色漆。或工业面漆。

Solvent composition溶剂组成

Butyl acetate   醋酸丁酯

Specifications规格

| Property性质 | Value规格 | Units单位 | Method方法 SBM * ISO |
| --- | --- | --- | --- |
| Non-volatiles 固体份 | 68 - 72 | % | 001G** 3251 |
| Acid value (as such)酸值 | 5.5 – 8.5 | mg KOH/g | 303A 3682 |
| Viscosity (23°C)黏度 at 50 s-1 | 1.5 – 3.5 | Pa.s | 012J 3219 |
| Colour (Lico 500)色泽 | Max. 50 | APHA | 008F 6271 |
| -OH Content(as such) 羟基含量（供应值） | 2.8-3.2 | % | 044B |
| Water content 水分含量 | <0.1 | % | 039A |
| Appearance外观 | clear, free of extraneous matter清澈透明无异物 |  | 017A |

* SBM:Nuplex Resins method of determination (available on request)

** spreading agent, methyl ethyl ketone

Typical properties典型特性

Density比重	:  1.03	kg/dm3	DIN 53217

Flash point闪点	:  22	°C	DIN 53213

Dilutability稀释性

Aliphatics  脂肪族：	white spirit           石油醚	not dilutable    不可稀释

Aromatics芳香族：	xylene                  二甲苯	dilutable          可稀释

Esters         酯类：	ethyl acetate        乙酸乙酯	dilutable          可稀释

butyl acetate        醋酸丁酯	dilutable          可稀释

Ketones      酮类：	acetone                丙酮	dilutable          可稀释

Compatibility相溶性

Desmodur N 75	 	+			Bayer AG

Desmodur L 75	 	+			Bayer AG

Desmodur N 3390	 	+			Bayer AG

Desmodur HL	 	+			Bayer AG

Desmodur IL    	 	+			Bayer AG

Tolonate HDB-75	 	+			Rhodia

Tolonate HDT-90	 	+			Rhodia

CAB 551-0.01	 	+			Eastman Kodak

Nitrocellulose ½ s	 	+			Hagedorn AG

Suitable mixing proportions (calculated on Non-volatiles) are marked +. Combinations in the proportions marked - are not recommended.

Package and store包装和贮存

200kg per steel drum.  200公斤钢桶包装.

Storage should be under cover, out of direct sunlight and avoiding extreme temperature changes.

Under normal storage conditions (5 – 35°C, away from extremes) sealed, unopened containers of this material would have a shelf life of 12 months from the date of manufacture. If it is stored for longer than 12 months, it is recommended that the product is rechecked for suitability in the intended application.

必须密封储存,避免阳光直接照射和极端的温度变化

在5-35°C密封条件下,从生产日期起保质期为十二个月,如果储存超过12个月后,建议对产品进行重新检测以适合于特定应用.